GLASS REINFORCED WALL COATING SYSTEM

DESCRIPTION

GRWCS is a fiberglass reinforced epoxy wall coating system. GRWCS provides a seamless wall-to-ceiling-to-floor surface that is easy to clean and maintain. Combining high impact and chemical resistance, GRWCS is the ideal wall system for use in commercial kitchens, clean rooms, operating rooms, and animal care facilities. Depending on weight of fiberglass used, installed thickness of GRWCS ranges from 6 to 40 mils. GRWCS can be incorporated into seamless floor cove base applications.

GRWCS is available with Bioclean for anti-microbial performance. Chemically resistant finish coats are available for the improved resistance of GRWCS-HP.

ADVANTAGES

- Low Odor for use in Occupied Areas (0-VOC)

- High Impact Resistance

- Seamless Surface Inhibits Bacteria Growth

- USDA Approved

- Easily Maintained

CONSIDERATIONS

- Substrate temperature must be a minimum of 50ºF.

- Substrate must be free of hydrostatic pressure, moisture transmission, paint, curing agents, and other foreign materials.

- Substrate irregularities will transmit through coating system.

APPLICATION

Surface Preparation

Surface Preparation is the most critical portion of any successful resinous flooring system application. All substrates must be properly prepared as outlined in the Company’s Technical Bulletin. Work must be performed by trained or experienced contractors or maintenance personnel.

Installation

GRWCS is installed over a smooth wall surface. Fiberglass cloth is imbedded into a base coat of Epoxy Wall Coating. Successive applications of specified finish coats are rolled over it to ensure a smooth surface and complete coverage of reinforcing fiberglass.

Clean Up

Clean skin with soap and water. Tools and equipment should be cleaned with xylene or lacquer thinner.

COMPOSITION

GRWCS is a 100% solids epoxy wall coating system reinforced with 2.6-7.5 ounce fiberglass cloth. 5.8 ounce fiberglass cloth reinforcement is the standard.

COLOR SELECTION

GRWCS is available in a variety of standard colors. Custom colors are available subject to laboratory approvals, minimum quantities, lead time for production, and increased cost.

TECHNICAL DATA

Coating System Performance Properties

| Flammability ASTM D-635 | Self Extinguishing over concrete |
| --- | --- |
| Fungus & Bacteria Growth MIL-F-52505 §4.4.2.11 | Will not support growth of fungus or bacteria when subjected to mildew and bacteria tests. |
| Hardness ASTM D-2240 | 70-80 Shore D |
| Bond Strength to Concrete ACI COMM #403 Bulletin 59 43 | 300-350 psi (100% concrete failure) |
| Flexibility ASTM C-522 | Passes 1” with no cracking |
| Water Absorption ASTM D-570 | 0.10% |
| Abrasion Resistance ASTM C-501 | 40 mg |
| Impact Resistance Gardner Impact Tester | >120 in/lbs |
| Tensile Strength ASTM C-307 | 9,000 psi |
| Thermal Coefficient of Expansion ASTM C-531 | 6-10 x 106 |

# Text boxes

CDF

Cole Diamond Flooring, Inc.

100 B Memorial Plaza

P.O. Box 866

Chestertown, MD 21620

410-810-0220 Office

410-810-0280 Fax

443-480-1172 Sales

TECHNICAL SERVICE

Cole Diamond Flooring (CDF) associates provide services and consultations on material selection, specification, troubleshooting, and other information on the proper repair and protection of concrete surfaces. CDF representatives are available to assist you at 410-810-0220.

AVAILABILITY

CDF flooring systems are available throughout the United States. Contact a representative for details.

MAINTENANCE

After completing the application of the Glass System the installer should provide the owner with maintenance instructions. If floors become slippery due to animal fats, oil, grease, or soap film, clean and rinse thoroughly.

Glass System is easily cleaned with neutral soaps or detergents. Routine mechanical scrubbing is recommended for all surfaces having a non-skid texture. Waxing is optional. Long periods of heavy traffic may cause wear patterns necessitating a maintenance application of a finish coat.

WARRANTY—CDF warrants for a period of one (1) year that its floors will be free of defects.  Material will be in conformity with published specifications when handled, stored, mixed and applied in accordance with recommendations. If any product fails to meet this warranty, the liability of CDF will be limited to replacement of any non-conforming material if notice of such non-conformity is given to CDF within (1) one year of delivery of materials. No one is authorized to make oral warranties on behalf of CDF. In order to obtain replacement or refund the customer must provide written notice containing full details of the non-conformity. CDF reserves the right to inspect the workmanship prior to replacement.