CDF DIVERSE EPOXY SYSTEM

Activity Centers

Aircraft Hangars

Airports Baggage/Service

Terminals

Animal Areas Housing

Cage Washing

Beverage Processing

Packaging/Warehouse Packaging/Warehousing

Bottling

Cafeterias

Chemical Processing

Clean Rooms

Coolers

Computer Assembly

Commercial Kitchens

Containment Areas

Convention Centers

Correctional Facilities

Corridors

Docks/Ramps

Dairies

Distilleries Packaging

Bottling

Food Processing

Preparation Service

Garages

Hospitals Corridors & Lobbies

Patient Rooms

Operating Rooms

Services

Laboratories

Laundries

Locker Rooms

Machine Shops

Manufacturing Light Duty

Heavy Duty

Meat, Fish, Poultry Processing

Mechanical Equipment Rooms

Munitions Facilities

Parking Garages Interior Decks

Exterior Decks

Pharmaceutical Plants

Pulp and Paper Processing Facilities

Schools

Shopping Malls

Showers

Utilities

Warehouses

Waste Water Treatment Facilities

DESCRIPTION

ADVANTAGES

CONSIDERATIONS

TECHNICAL DATA

System Performance Properties

| Flammability ASTM D-635 | Self Extinguishing |
| --- | --- |
| Fungus & Bacteria Growth MIL-F-52505 §4.4.2.11 | Will not support growth of fungus or bacteria when subjected to mildew and bacteria tests. |
| Hardness ASTM D-2240 | 70-75 to 80-84 Shore D |
| Bond Strength to Concrete ACI COMM #403 Bulletin 59 43 | 300 psi to 400 psi (100% concrete failure) |
| Resistance to Elevated Temperature MIL-D-3134F§4.7.4 | No slip or flow at required temperature of 158°F |
| Coefficient of Friction ASTM D-2047 | 0.80 |
| Water Absorption ASTM D-570 | Nil |
| Thermal Shock Resistance ASTM C-884 | Passes |
| Abrasion Resistance ASTM D4060 | 32 to 50 mg |
| Impact Resistance MIL-D-3134F §4.7.3 | Withstands 16 ft/lbs. without cracking, delamination, or chipping |
| Compressive Strength ASTM C-579, 7 days | 10,000 to 14,000 psi minimum |
| Tensile Strength ASTM C-307 | 2,400 to 2,600 psi |
| Thermal Coefficient of Expansion ASTM C-531 | 22 x 106 to 26 x 106 |
| Adhesive Strength MIL-D-26413 | 420 psi |
| Flexural Strength ASTM C-580 | 4,300 psi |

APPLICATION

MAINTENANCE

# Text boxes

CDF

Cole Diamond Flooring, Inc.

100 B Memorial Plaza

P.O. Box 866

Chestertown, MD 21620

410-810-0220 Office

410-810-0280 Fax

443-480-1172 Sales

CDF DIVERSE EPOXY SYSTEM is a fluid applied resin flooring system consisting of 100% solids epoxy and graded aggregates that provide a Floor System from 10 mils to 1/4” thick. CDF DIVERSE EPOXY SYSTEM produces a dense, chemical resistant, skid-inhibiting finish that will minimize maintenance and provide a durable finish. It can also be modified for thermal shock.

CDF DIVERSE EPOXY SYSTEM can have a variety of decorative finishes including colored quartz or vinyl chips (see color charts).   Our system is designed to enhance the chemical resistance, abrasion resistance, gloss retention, and non-skid properties. CDF DIVERSE EPOXY SYSTEM can have an additional non-skid added as part of the final seal coat (aluminum oxide).

CDF DIVERSE EPOXY SYSTEM can be installed with an integral cove base for areas requiring seamless wall to floor coatings. A waterproof crack-resistant system can be achieved by using a waterproofing membrane.

SELECTION GUIDE

- Thermal Shock Resistant

- High Wear, Impact and Abrasion Resistance

- Low Maintenance

- Safe (non-skid)

- Chemical Resistant Finishes are Available

- 100% Solids Provides Low Odor Application

- On or below grade installation must have an efficient vapor barrier under the slab.

- Special treatments are necessary where hydrostatic pressure or moisture vapor transmission may be present.

- Substrate temperature must be a minimum of 55°F (low temperature cure system available on request).

- Substrate must be free of dirt, waxes, curing agents and other foreign materials.

- All control joints and expansion joints in the substrate must be revealed with the appropriate divider strips in the topping.

WARRANTY—CDF warrants for a period of one (1) year that its floors will be free of defects.  Material will be in conformity with published specifications when handled, stored, mixed and applied in accordance with recommendations. If any product fails to meet this warranty, the liability of CDF will be limited to replacement of any non-conforming material if notice of such non-conformity is given to CDF within (1) one year of delivery of materials. No one is authorized to make oral warranties on behalf of CDF. In order to obtain replacement or refund the customer must provide written notice containing full details of the non-conformity. CDF reserves the right to inspect the workmanship prior to replacement.

COMPOSITION

Some systems are 100% solids clear epoxy resin with decorative colored quartz aggregates. Urethane and epoxy finish coats provide specific performance characteristics. Mortar systems are composed of 100% solids epoxy resin filled with a variety of graded quartz and silica fillers that can be modified to create the best design mix for ideal performance. A wide selection of finish coats is available to meet various exposure requirements.

COLOR & AVAILABILITY

COLE DIAMOND DIVERSE EPOXY SYSTEMs are available in a variety of standard blends of colored quartz. Colors will not fade or wear thin.

Flooring systems are available throughout the United States.

TECHNICAL SERVICE

We provide services and consultations on material selection, specification, troubleshooting, and other information on the proper repair and protection of concrete surfaces.

After completing the application of a COLE DIAMOND DIVERSE EPOXY SYSTEM, the installer should provide the owner with maintenance instructions. If floors become slippery due to animal fats, oil, grease, or soap film, clean and rinse thoroughly.

COLE DIAMOND DIVERSE EPOXY SYSTEMs are easily cleaned with neutral soaps or detergents. Routine mechanical scrubbing is recommended for all surfaces having a non-skid texture. Waxing is optional. Long periods of heavy traffic may cause wear patterns necessitating a maintenance application of a finish coat.

Concrete surfaces must be in sound condition and properly prepared prior to any flooring system installation. Refer to technical bulletin for specific preparation guidelines.

Installation of COLE DIAMOND DIVERSE EPOXY SYSTEM involves several steps including priming, applying (or troweling) successive base coats, broadcasting color quartz, grouting, and sealing. For specific installation guidelines consult the instruction manual.

Neat Resin

Performance Properties

Neat Resin

Performance Properties

Compressive Strength

ASTM D-695                               13,000 psi

Ultimate Tensile Strength

ASTM D-638                                 4,200 psi

Tensile Elongation

ASTM D-638                                    6-8%

Flexural Strength

ASTM D-790                                 7,800 psi

Flexural Modulus                       2.5 x105  or

ASTM D-790                             6.4 x 105

Hardness

ASTM D-2240                      65-85 Shore D

COMPOSITION

Some systems are 100% solids clear epoxy resin with decorative colored quartz aggregates. Urethane and epoxy finish coats provide specific performance characteristics. Mortar systems are composed of 100% solids epoxy resin filled with a variety of graded quartz and silica fillers that can be modified to create the best design mix for ideal performance. A wide selection of finish coats is available to meet various exposure requirements.

COLOR & AVAILABILITY

COLE DIAMOND DIVERSE EPOXY SYSTEMs are available in a variety of standard blends of colored quartz. Colors will not fade or wear thin.

Flooring systems are available throughout the United States.

TECHNICAL SERVICE

We provide services and consultations on material selection, specification, troubleshooting, and other information on the proper repair and protection of concrete surfaces.

Concrete surfaces must be in sound condition and properly prepared prior to any flooring system installation. Refer to technical bulletin for specific preparation guidelines.

Installation of COLE DIAMOND DIVERSE EPOXY SYSTEM involves several steps including priming, applying (or troweling) successive base coats, broadcasting color quartz, grouting, and sealing. For specific installation guidelines consult the instruction manual.

After completing the application of a COLE DIAMOND DIVERSE EPOXY SYSTEM, the installer should provide the owner with maintenance instructions. If floors become slippery due to animal fats, oil, grease, or soap film, clean and rinse thoroughly.

COLE DIAMOND DIVERSE EPOXY SYSTEMs are easily cleaned with neutral soaps or detergents. Routine mechanical scrubbing is recommended for all surfaces having a non-skid texture. Waxing is optional. Long periods of heavy traffic may cause wear patterns necessitating a maintenance application of a finish coat.

WARRANTY—CDF warrants for a period of one (1) year that its floors will be free of defects.  Material will be in conformity with published specifications when handled, stored, mixed and applied in accordance with recommendations. If any product fails to meet this warranty, the liability of CDF will be limited to replacement of any non-conforming material if notice of such non-conformity is given to CDF within (1) one year of delivery of materials. No one is authorized to make oral warranties on behalf of CDF. In order to obtain replacement or refund the customer must provide written notice containing full details of the non-conformity. CDF reserves the right to inspect the workmanship prior to replacement.