635 MVT

MOISTURE VAPOR TREATMENT

DESCRIPTION

635 MVT is a two component modified epoxy system designed to seal concrete and reduce moisture

vapor transmission prior to applying finished flooring.

635 MVT has proven to reduce moisture vapor emissions and be resistant to damage from high

alkalinity.

635 MVT is an environmentally friendly material containing no hydrocarbons or other solvents making

it zero (0) VOC.

ADVANTAGES

• Reduces moisture vapor transmission rate through concrete.

• Provides excellent resistance to highly alkaline conditions.

• Gives excellent bond to properly prepared concrete.

• Has convenient 2:1 mixing ratio.

• High physical properties.

• Can be rapidly surfaced with a variety of finished flooring materials.

CONSIDERATIONS

• Substrate temperature must be a minimum of 55oF before, during and 72 hours after installation.

• Must have effective vapor barrier directly under substrate.

• For use only on properly prepared surfaces; must be free of dirt, waxes, curing agents and other

foreign materials.

• Does not function as a crack reflective membrane.

TYPICAL USES

635 MVT is designed as a negative side moisture vapor retarder to reduce moisture vapor

transmission through concrete.

635 MVT can also be an effective primer for fast recoat under a flooring system

COMPOSITION

635 MVT is a highly cross-linked, alkaline resistant epoxy composition.

TECHNICAL DATA

Coating System Performance Properties

| Tensile Strength ASTM D-638 | 10,400 psi |
| --- | --- |
| Tensile Elongation ASTM D-638 | 2-4% |
| Modulus of Elasticity ASTM D-638 | 2500 psi |
| Hardness Shore D ASTM D-2240 | 85 |
| Bond Strength to Concrete ASTM D-4541 | 400-450 psi (100% concrete failure) |
| Permeability ASTM E-96 | 1 coat (10-12 mils) 0.081 Perms 2 coats (20 mils total) 0.040 Perms |
| Water Vapor Transmission ASTM E-96 Grams/hr/sq. meter | 1 coat 0.023 2 coat 0.012 |
| Alkaline Resistance ASTM D-1308 7 day immersion 14 day immersion | 10% sodium hydroxide-unaffected 50% sodium hydroxide-unaffected 10% sodium hydroxide-unaffected 50% sodium hydroxide-unaffected |
| VOC | zero |
| Water Absorption ASTM D-570 | nil |
| Mix Ratio | 2:1 by volume |
| Pot Life | 25-35 minutes |
| Recoat Time Minimum/Maximum | 4-6 hrs/72 hrs |

MIXING & SPREADING

Stir resin and hardener separately prior to mixing. Mix ratio is 2 parts resin Part A to one part hardener Part B. Pour together and mix thoroughly for 60-90 seconds. Apply at the rate of 120-130 sq. ft./gal. Apply extra material to areas showing penetration and soaking into the concrete. All areas should show a uniform gloss and a uniform 12 mils minimum thickness.

Maximum recoat time for 635 MVT is 72 hours. It may be advantageous to prime with 502 primer or a second coat of 635 MVT at 200-250/sq.ft. and lightly broadcast 30 mesh silica to help achieve a good mechanical bond.

For areas showing moisture vapor greater than 12#/1000sq.ft/24 hours or humidity readings greater than 95% consult with the Technical Department.

AVAILABILITY

CDF flooring systems are available throughout the United States. Contact a representative for details.

TECHNICAL SERVICE

Cole Diamond Flooring provides service and consultation on material selection, specification, troubleshooting, and other information on the proper repair and protection of concrete surfaces. Call 410-810-0220.

# Text boxes

CDF

Cole Diamond Flooring, Inc.

100 B Memorial Plaza

P.O. Box 866

Chestertown, MD 21620

410-810-0220 Office

410-810-0280 Fax

443-480-1172 Sales

WARRANTY—CDF warrants for a period of one (1) year that its floors will be free of defects.  Material will be in conformity with published specifications when handled, stored, mixed and applied in accordance with recommendations. If any product fails to meet this warranty, the liability of CDF will be limited to replacement of any non-conforming material if notice of such non-conformity is given to CDF within (1) one year of delivery of materials. No one is authorized to make oral warranties on behalf of CDF. In order to obtain replacement or refund the customer must provide written notice containing full details of the non-conformity. CDF reserves the right to inspect the workmanship prior to replacement.

APPLICATION

Surface Preparation

Surface preparation is the most critical portion of any successful resinous flooring system. All substrates must be properly prepared as outlined in the Technical Bulletin . Work must be

performed by trained or experienced contractors or maintenance personnel.

635 MVT is a moisture vapor suppressant for concrete substrates. Surface and air temperature must be a minimum of 55oF during installation and cure.

Concrete surface must be free of dirt, waxes, curing agents, any other foreign materials, and must be structurally sound. Surfaces should be vacuum shot blasted to “open” surface porosity or by diamond grinding with coarse stones. Surface profile must be a minimum CSP-4-CSP-5 profile according to International Concrete Repair Institute Guideline #03732.

Concrete surfaces should be tested for moisture transmission according to ASTM-F-2170 (Relative Humidity in Concrete Floor Slabs using in situ probes) and ASTM-F-1869 (Measuring Moisture Vapor Emission Rate of Concrete Subfloor using Anhydrous Calcium Chloride).

635 MVT may be applied in a single coat of 12 mils (130 sq. ft. per gallon) when relative humidity readings are below 95% or MVT readings are below 12# per 1000 sq.ft./24 hrs. Higher readings require consultation with Technical Services and may require a second coat of 635 MVT of 10 mils (160 sq.ft. per gallon).

Fill all cracks and non-moving joints with 635 MVT. If material continues to disappear into the void, add fumed silica to get a gel consistency and “putty” into the void to completely seal. Detailing with membrane and glass mesh is done after the 635 MVT application.

WARRANTY—CDF warrants for a period of one (1) year that its floors will be free of defects.  Material will be in conformity with published specifications when handled, stored, mixed and applied in accordance with recommendations. If any product fails to meet this warranty, the liability of CDF will be limited to replacement of any non-conforming material if notice of such non-conformity is given to CDF within (1) one year of delivery of materials. No one is authorized to make oral warranties on behalf of CDF. In order to obtain replacement or refund the customer must provide written notice containing full details of the non-conformity. CDF reserves the right to inspect the workmanship prior to replacement.